Device

- Name:				PANalytical Empyrean

X-ray tube

- Anode material:		Co

- Voltage (kV):			35

- Current (mA):			35

Filter

- Name:				Beta-filter Iron

Detector

- Name:				PIXcel3D-Medipix3 1x1 detector

- Type:				Area detector

Scan

- Scan range (°):			5.0 – 80.0

- Step size (°):			0.0131

- Radiated sample area:		15.0 x 12.0 mm

- Measurement time: 		153 min

Software

- phase identification (qualitative XRD) based on ICDD PDF-5+2026 database and PANalytical HighScore 3.0.4 program

- (semi-) quantitative phase identification: Profex 5.1.0 software -- using Rietveld refinement (cite: Döbelin and Kleeberg, 2015, https://doi.org/10.1107/S1600576715014685)

XRD – sample preparation

- about 2.5 ml sample (ca. 0.4 mg Al2O3 + 1.6 mg sample <400 µm) was ground together with 10 ml Ethanol and grinding elements made of zirconium dioxide by using the XRD-Mill McCrone from Retsch

- after milling the sample was poured with about 40 ml ethanol into a petri dish and air dried over night

- the dried sample was homogenized with small steel balls (4 mm diameter) by using the mixer mill MM 400 from Retsch

- the sample was prepared into the sample holders (24/27 mm diameter) by using the backloading method and measured (see device parameters)